## Slide 1: Bio-inspired synthesis, characterization and biomedical applications of optimized silver nanoparticles functionalized with Ceiba pentandra (L.) Gaertn. (Kapok tree)
Presented by
Dr. Loick P. KOJOM FOKO, Ph.D.
ECR & Lecturer
(Biotechnology – Microbiology – Epidemiology)
CAiSMD WORKSHOP
27th – 29th February 2024,
University of Buea, Cameroon
Loick Pradel Kojom Foko,1,2,* Joseph Hawadak,1,2 Vaishali Verma,3 Philippe Belle Ebanda Kedi,4 Raghavendra Kamaraju,3 Veena Pande,2 and Vineeta Singh1,*
1Parasite and Host Biology Group, National Institute of Malaria Research, New-Delhi, India 2Department of Biotechnology, Kumaun University, Bhimtal, India
3Vector Biology Group, National Institute of Malaria Research, New-Delhi, India
4Department of Pharmaceutical Sciences, The University of Douala, Douala, Cameroon

## Slide 2
OUTLINE
Introduction
Objectives
Materials and Methods
Results and Discussion
Conclusions
Acknowledgments

## Slide 3
Introduction (1/4)
Pathogen: Parasite protozoan (Plasmodium)
Arthropod-borne disease (Anophelinae female mosquito)
Other routes: Blood transfusion, congenital
Five human Plasmodium : P. falciparum (Pf), P. vivax (Pv), P. malariae (Pm), P. ovale spp (Po) and P. knowlesi (Pk)
Malaria disease
Fig. 1. Lifecycle of human Plasmodium sp parasites
Source: Davies et al., 2017,
Cowman et al., 2016

## Slide 4
Introduction (2/4)
About 249 millions cases and 608,000 deaths
Mainly due to Pf
Pv accounts for ~3% of global cases
sSA accounted for > 90% of cases and deaths
Malaria situation in 2022
Fig. 2. Worldwide burden of malaria in 2022
Source: WHO, 2023

## Slide 5
Introduction (3/4)
Fig. 3. Malaria case incidence (a) and mortality rate (b) in the WHO African Region, 2019
Large decrease in malaria morbidity and mortality these last two decades
Implementation and scale up of control measures (LLINs, IRS, RDTs, IPTp, SMC, ACTs)
Malaria still remain an important public health concern especially in Cameroon & India
Cocktail of reasons: Self-medication, asymptomatic malaria, low (very low) parasitemia, mosquito resistance, deletions in the pfhrp2 gene, COVID-19, drug resistance, etc.

## Slide 6
Introduction (4/4)
Chloroquine/
Quinine
Sulfadoxine - Pyrimethamine
ACTs
Artesunate + Amodiaquine
Artemether + Lumefantrine
Artesunate + SP
Artesunate + Mefloquine
Artesunate + Pyronaridine
Dihydroartemisinin + Piperaquine
Proguanil
Primaquine
Tafenoquine
Halofantrine
Emergence and spread of Pf parasites resistant to ACTs as seen recently in Africa (Rwanda, Uganda, Sudan)
Source: WHO, 2023
Searching and developing alternative drugs using innovative approaches
Source: Uwimana et al., 2021
Balikagala et al., 2021
Fola et al., 2023

## Slide 7
Objectives (1/1)
To synthesize, optimize, and characterize Ceiba pentandra-synthesized silver nanoparticles (CP-AgNPs);
To evaluate the hemocompatibility potential of CP-AgNPs;
To evaluate the antiplasmodial potential of CP-AgNPs against P. falciparum;
To evaluate the larvicidal potential of CP-AgNPs against Aedes aegypti, Culex quinquefasciatus and Anopheles stephensi.

## Slide 8
MATERIALS AND METHODS

## Slide 9
Materials and Methods (1/9)
Treatment part
Plant collection and ethnobotanical identification
Ceiba pentandra
Malvaceae
Domesticated in Cameroon
Nutritional purposes
Skin diseases, diarrhea, bronchitis
Collected in Douala (Cameroon) and Identified at the National Herbarium of Cameroon
Fig. 4. Ceiba pentandra (Plant & Leaves)

## Slide 10
Materials and Methods (2/9)
Fig. 5. Flow diagram of the study

## Slide 11
Materials and Methods (3/9)
Aqueous plant extract preparation
Fresh leaves
Powder
Decoction (80°C, 5 min)
Washing
Cutting
Drying
Grounding
Powder
(10 g)
Distilled water
(100 mL)
Cooling at room temperature
Storage (4°C)
Filtration
Whatman N°1 paper
Fig. 6. Preparation of the plant extracts

## Slide 12
Materials and Methods (4/9)
Nanoparticle synthesis & Optimization
Plant extract
Silver nitrate
(AgNO3)
Silver nanoparticles
Fig. 7. Synthesis and optimization of NPs

## Slide 13
Materials and Methods (5/9)
Plant extract and Nanoparticle characterization
Table. 1. Methods used to characterize substances
Substances | Methods | Parameters evaluated
Extracts | Gas Chromatography + Mass spectrometry (GC-MS) | Phytochemical profile
Nanoparticles | Ultraviolet-Visible spectroscopy (UV-Vis) | Surface plasmon resonance
 | Electron microscopy (TEM & SEM) | Shape, size, size distribution
 | Energy dispersed X-ray (EDX) | Atom content
 | Fourier transformed infrared spectroscopy (FTIR) | Functional chemical groups
 | X-ray/Selected area electron diffraction (XRD/SAED) | Structure/Crystallinity
 | Zeta potential | Stability
 | Dynamic light scattering (DLS) | size, size distribution

## Slide 14
Materials and Methods (6/9)
Hemolysis assay
Fig. 8. Summary of hemolysis assay
Washing with incomplete medium
Dilution with PBS
Blood
(Hct = 35%)
Blood
(Hct = 1%)
Tubes – 1.5 µL
(Vt = 200 µL)
180 µL
20 µL
Different substances
PBS (NC)
Saponin (PC)
AgNPs
CQ (standard drug)
Incubation at 37°C for 30 min and 24 hrs
Triplicate
Centrifugation
(3000g, 4 min)
100 µL
Transfer to 96-well plate
Spectrophotometry
540 nm
Source: Wang et al., 2010
Supernatant

## Slide 15
Materials and Methods (7/9)
Antiplasmodial assay
Fig. 9. Summary of antiplasmodial assay
Introduction of CE, AgNPs, and CQ
Mixing up 10 µL of synchronized blood with the substances tested
Incubation at 37°C for
48 hours
Adding lysis buffer, 1h dark incubation, and reading

## Slide 16
Materials and Methods (8/9)
Larvicidal assay
Fig. 10. Summary of
larvicidal assay
Mosquito rearing
Distribution of larvae
Larvicidal effect after 24h, 48h, and 75h exposure
Batches of 100 eggs into 18 cm × 13 cm × 4 cm trays (500 mL of water),
Conditions: 27°C, 75–85%, and light/dark photoperiod (h/h): 14/10
Eggs were fed daily with TetraBits fish food
Instar 3rd and 4th larvae obtained were used to perform larvicidal assays.
Introduction of NPs, Extract, Controls at different concentrations

## Slide 17
Materials and Methods (9/9)
Statistical analysis
StatView v5.0, SPSS v22, and GraphPad v8.03
Qualitative variables = percentage/95%CI - Quantitative variables = mean ± SD
A probit model was used to analyze dose/time mortality response data from larvicidal assays, and determine LC50 and LC90 and their confidence intervals at 95% (95% CI).
The Abbott’s formula was used to correct the mortality rate if it comprised between 5% and 20% in the negative control (NC) group
One-way analysis of variance (ANOVA), Pearson’s independence chi-square, and McNemar’s tests
Statistical significance threshold of 5%

## Slide 18
RESULTS AND DISCUSSION

## Slide 19
Results and Discussion (1/11)
Three compounds namely
2-Hexadecen-1-ol, 3,7,11,15-tetramethyl-, [R-[R*,R*-(E)]]-,
Lup-20(29)-en-3-one,
2,3-Dihydro-benzofuran were predominantly represented at proportion of 22.3%, 11.41% and 8.12%, respectively
Peak# | Retention time | Area% | Name of the compounds
1 | 7.39 | 0.78 | Benzene, 1,3-bis(1,1-dimethylethyl)-
2 | 8.62 | 8.12 | 2,3-Dihydro-benzofuran
3 | 10.90 | 0.45 | (Z)-1-Methyl-4-(6-methylhept-5-en-2-ylidene)cyclohex-1-ene
4 | 12.12 | 2.08 | 1,2-Benzenedicarboxylic acid, diethyl ester
5 | 12.83 | 0.56 | 2-[2-[2-(2,2,3,3,3-Pentafluoropropanoyl)oxyethoxy]ethoxy]ethyl 2,2,3,3,3-pentafluoropropanoate
6 | 13.72 | 1.47 | Trans-3(10)-caren-2-ol
7 | 14.61 | 2.71 | Neophytadiene
8 | 14.87 | 0.65 | 3H-3,10a-Methano-1,2-benzodioxocin-3-ol, octahydro-7,7-dimethyl-, (3.alpha.,6a.beta.,10a.beta.)-
9 | 15.07 | 2.07 | 2-N-Dodecylcyclohexanone
10 | 15.97 | 5.57 | Dibutyl phthalate
11 | 17.34 | 22.3 | 2-Hexadecen-1-ol, 3,7,11,15-tetramethyl-, [R-[R*,R*-(E)]]-
12 | 18.22 | 1.37 | Carbonic acid, but-3-yn-1-yl octadecyl ester
13 | 19.49 | 0.82 | 4,8,12,16-Tetramethylheptadecan-4-olide
14 | 20.94 | 3.4 | 2-Dodecylcyclobutanone
15 | 24.73 | 0.52 | .gamma.-Tocopherol
16 | 25.13 | 1.9 | 4,4,6a,6b,8a,11,11,14b-Octamethyl-1,4,4a,5,6,6a,6b,7,8,8a,9,10,11,12,12a,14,14a,14b-octadecahydro-2H-picen-3-one
17 | 25.56 | 1.7 | D:A-Friedoolean-6-ene
18 | 26.08 | 2.98 | 2H-2,4a-Ethanonaphthalen-8(5H)-one, hexahydro-2,5,5-trimethyl
19 | 26.50 | 0.78 | Ursa-9(11),12-dien-3-one
20 | 27.32 | 3.19 | .gamma.-Sitosterol
21 | 27.48 | 3.71 | 4,4,6A,6B,8A,11,11,14B-Octamethyl-1,4,4A,5,6,6A,6b,7,8,8a,9,10,11,12,12a,14,14a,14b-octadecahydro-2H-picen-3-one
22 | 27.87 | 5.57 | A'-Neogammacer-22(29)-ene
23 | 28.06 | 11.41 | Lup-20(29)-en-3-one
24 | 28.29 | 2.61 | 2-Butanone, 4-(2,2-dimethyl-6-methylenecyclohexylidene)-3-methyl-, (Z)-
25 | 28.44 | 7.61 | Lupeol
26 | 30.67 | 4.57 | Olean-12-en-28-oic acid, 2.beta.,3.beta.,23-trihydroxy-, methyl ester
27 | 33.18 | 1.11 | 9,19-Cyclo-9.beta.-lanostane-3.beta.,25-diol

## Slide 20
Results and Discussion (2/11)
Brown (CP)
A rapid color change (less than 10 minutes) was observed upon mixing plant extracts with AgNO3 aqueous solution.
This change indicates the AgNPs synthesis through reduction of Ag+ ions present in solution by reducing agents contained in CEs.
Fig. 11. Color changes showing synthesis of CP-AgNPs

## Slide 21
Results and Discussion (3/11)
Optimization: C. pentandra
Concentration (AgNO3) = 4 mM, Incubation time = 4 hours, Incubation temperature = 85°C,
Extract plant/AgNO3 ratio of 1: 9
Absorption peak was observed at 430 nm for CP-AgNPs.
This result translates the phenomenon of surface plasmon resonance (SPR) which occurs after bioreduction of Ag+ ions, and due to the excitation of electrons present on the NPs surface which enter into resonance with the wavelength of the incident light.
Fig. 12. Optimization of AgNPs synthesis

## Slide 22
Results and Discussion (4/11)
SEM and TEM micrographs confirmed that NPs of each plant were mainly spheroidal in shape with low polydispersity. Consistent with earlier studies with plants such as Azadirachta indica, Barletia cristata, Berberis tinctoria and Holostemma ada-kodien (Chandramohan et al., 2015; Govindarajan et al., 2016; Mahesh Kumar et al., 2016; Alyahya et al., 2018)
Fig. 13. TEM and SEM analysis of CP-NPs
SEM
TEM

## Slide 23
Results and Discussion (5/11)
Strong SILVER signal
Other signals (Oxygen, Cadmium, Chloride, Phosphorus, Silica, Calcium)
Presence in plant extracts as confirmed by GC-MS analysis
Source: Kojom Foko et al., 2019; 2020
Fig. 14. EDX analysis of CP-NPs

## Slide 24
Results and Discussion (6/11)
Fig. 15. XRD and FITR of CP-NPs
Crystalline nature of NPs with a face-centered structure
peaks corresponding to the (111), (200), (220) and (311) sets of the lattice planes.
Different vibrations
3403 cm-1: OH- stretch (polyphenols, polysaccharides, proteins)
1454 cm-1 : C=C stretch, C-H bend (Aromatic compounds such as flavones and terpenoids)

## Slide 25
Results and Discussion (7/11)
Fig. 16. Zeta potential and DLS analysis of CP-NPs
AgNPs were highly stable and this outlines the absence of phenomena such as aggregation and flocculation which characterize an instability of NPs and can greatly influence their properties (Cui et al., 2012).

## Slide 26
Results and Discussion (8/11)
Hemolysis rate is dose-, and time-dependent for all substances
CP-AgNPs had HC50 comprised between 250 to 500 µg/mL
Fig. 17. Hemotoxic effects of AgNPs after 30 minutes (a) and 24 hours (b)

## Slide 27
Results and Discussion (9/11)
NPs more effective than CE
NPs are highly effective (IC50 ≤ 20 µg/mL)
AgNPs more effective on 3D7 Compared to RKL9
Table. 2. Antiplasmodial activity of CP-AgNPs against 3D7 and RKL9
Overall, our biosynthesized NPs were more effective than those reported in earlier studies (Kojom Foko et al., 2019)
A cocktail of factors (size, shape, metal source and chemical compounds) could explain these discrepancies between studies.
NPs could provoke Plasmodium death by acting on multiple targets including enzymes, cell membrane and internal organelles (Kamaraj et al., 2017; Varela Aramburu et al., 2020)

## Slide 28
Results and Discussion (10/11)
Table. 3. Larval toxicity of the CP–CE and CP–AgNPs against mosquitoes after 24h, 48h and 72 exposure

## Slide 29
Results and Discussion (11/11)
Figure. 18. Morphological deformities induced by the exposure to CP–AgNPs (LC50 dose) on larval stages of Ae. aegypti, Cx. quinquefasciatus, and An. stephensi.
CP–AgNPs elicited a multitude of morphological changes on mosquito larvae which comprised of pigmentation of body, swelling of the apical cells, necrosis and thickening of the epidermis, loss of external hairs/bristles, and shrinkage of the larvae

## Slide 30
CONCLUSIONS

## Slide 31
Conclusions (1/1)
The synthesis was rapid and the biosynthesized AgNPs were polycrystalline, mostly spherical, well dispersed and stable with the role of plant compounds such as alcohols and amides as reducing and/or capping agents.
AgNPs were highly potent against Pf growth with low toxicity against RBCs thereby outlining a good hemocompatibility.
AgNPs were highly potent against mosquito larvae

## Slide 32
AKNOWLEDGMENTS

## Slide 33
Acknowledgments (1/2)

## Slide 34
Acknowledgments (2/2)
Dr Vineeta Singh
Scientist ‘E’ & PI
Prof. Veena Pande
Full professor & PI
Dr Raghavendra Kamaraju
Former Scientist ‘G’ & PI
Dr Vaishali Verma
Scientist ‘C’
Dr. Philippe Belle Ebanda Kedi
Assistant lecturer
Mr. Joseph Hawadak
Senior Research Fellow
PARASITE
VECTOR